## Slide 1: Finite Element Analysis of pipe
Samer Adeeb
May 2014
Effect of Properties and Geometry on Buckling Response

## Slide 2: Background
Ph.D. Structural Engineering 2005. University of Calgary
TSTM, TCPL August 2004 – December 2006

## Slide 3: Outline
Introduction – Loads on pipelines
Introduction – Finite Element Analysis
Internal Pressure and Bending in Cold Bends
Material Properties of HSS Pipes
  Anisotropy models
  Anisotropy and Buckling
Initial Imperfections of HSS Pipes
  Measurement of Initial Imperfections
  Initial Imperfections and Buckling

## Slide 4: Intro: Loads on Pipe
Internal Pressure
  Theoretical:

## Slide 5: Intro: Loads on Pipe
Internal Pressure
  Theoretical:
  Barlow Formula:

## Slide 6: Intro: Loads on Pipe
Internal Pressure
  Theoretical:
  Barlow Formula:
  Exact:
Geometric Nonlinearity!

## Slide 7: Intro: Loads on Pipe
Lateral Loads
http://www.neb-one.gc.ca/clf-nsi/rthnb/pplctnsbfrthnb/mcknzgsprjct/rfd/rfdv1p3-eng.html#p3s5

## Slide 8: Intro: Loads on Pipe
Lateral Loads
http://www.neb-one.gc.ca/clf-nsi/rthnb/pplctnsbfrthnb/mcknzgsprjct/rfd/rfdv1p3-eng.html#p3s5

## Slide 9: Intro: loads on pipe
Lateral Loads. Thermal Expansion and Upheaval Buckling
http://wiki.iploca.com/display/rtswiki/Appendix+6.2+-+Pipeline+Trench+Design

## Slide 10: Intro: Loads on Pipe
Lateral Loads & Internal Pressure

## Slide 11: Intro: Loads on Pipe
Lateral Loads & Internal Pressure
Complex Interaction!

## Slide 12: Intro: FEA
What is FEA?
  Problem:
  Exact Solution:
  The following are Numerical Approximate Solutions:

## Slide 13: Intro: FEA
What is FEA?

## Slide 14: Intro: FEA
What is FEA?

## Slide 15: Intro: FEA
What is FEA?

## Slide 16: Intro: FEA
What is FEA?

## Slide 17: Intro: FEA
What is FEA?

## Slide 18: Intro: FEA
What is FEA?

## Slide 19: Internal Pressure and Bending in Cold Bends
Combined Load Experiments
[1] Sen, M. (2006); “Behaviour of Cold Bend Pipes Under Combined Loads” Ph.D. dissertation, University of Alberta, 2006
[2] Sen, M., Cheng, J.J.R., Zhou, J. (2011); “Behaviour of Cold Bend Pipes under Bending Loads”
DOI: 10.1061/(ASCE)ST.1943-541X.0000219. 2011 American Society of Civil Engineers

## Slide 20: Internal Pressure and Bending in Cold Bends
Model
Load
Cakiroglu, C.; Kainat, M.; Adeeb S.; Cheng, J.J.R. and Sen, M. (2014). Evaluation of Pressurized Cold Bend Pipe Body Tensile Fractures Under Bending Loads. Proceedings of the International Pipeline Conference (IPC 2014), September 29-October 3, Calgary, Alberta, Canada.
NPS30, t=8.29mm

## Slide 21: Internal Pressure and Bending in Cold Bends
Compression vs. Tension Failure
20%SMYS
Cakiroglu, C.; Kainat, M.; Adeeb S.; Cheng, J.J.R. and Sen, M. (2014). Evaluation of Pressurized Cold Bend Pipe Body Tensile Fractures Under Bending Loads. Proceedings of the International Pipeline Conference (IPC 2014), September 29-October 3, Calgary, Alberta, Canada.

## Slide 22: Internal Pressure and Bending in Cold Bends
Compression vs. Tension Failure
67%SMYS
Cakiroglu, C.; Kainat, M.; Adeeb S.; Cheng, J.J.R. and Sen, M. (2014). Evaluation of Pressurized Cold Bend Pipe Body Tensile Fractures Under Bending Loads. Proceedings of the International Pipeline Conference (IPC 2014), September 29-October 3, Calgary, Alberta, Canada.

## Slide 23: Internal Pressure and Bending in Cold Bends
Compression vs. Tension Failure
20%SMYS
67%SMYS
Cakiroglu, C.; Kainat, M.; Adeeb S.; Cheng, J.J.R. and Sen, M. (2014). Evaluation of Pressurized Cold Bend Pipe Body Tensile Fractures Under Bending Loads. Proceedings of the International Pipeline Conference (IPC 2014), September 29-October 3, Calgary, Alberta, Canada.

## Slide 24: Internal Pressure and Bending in Cold Bends
Compression vs. Tension Failure
20%SMYS
67%SMYS
Cakiroglu, C.; Kainat, M.; Adeeb S.; Cheng, J.J.R. and Sen, M. (2014). Evaluation of Pressurized Cold Bend Pipe Body Tensile Fractures Under Bending Loads. Proceedings of the International Pipeline Conference (IPC 2014), September 29-October 3, Calgary, Alberta, Canada.

## Slide 25: Internal Pressure and Bending in Cold Bends
Transition Pressure
Tension Side Fracture
Cakiroglu, C.; Kainat, M.; Adeeb S.; Cheng, J.J.R. and Sen, M. (2014). Evaluation of Pressurized Cold Bend Pipe Body Tensile Fractures Under Bending Loads. Proceedings of the International Pipeline Conference (IPC 2014), September 29-October 3, Calgary, Alberta, Canada.

## Slide 26: Internal Pressure and Bending in Cold Bends
Transition Pressure and Grade
Cakiroglu, C.; Kainat, M.; Adeeb S.; Cheng, J.J.R. and Sen, M. (2014). Evaluation of Pressurized Cold Bend Pipe Body Tensile Fractures Under Bending Loads. Proceedings of the International Pipeline Conference (IPC 2014), September 29-October 3, Calgary, Alberta, Canada.

## Slide 27: Internal Pressure and Bending in Cold Bends
Future Work
  Effect of Stress Strain Curve
  Different OD and t
  Straight pipes

## Slide 28: Material Properties of HSS Pipes
Anisotropy

## Slide 29: Material Properties of HSS Pipes
Anisotropy

## Slide 30: Material Properties of HSS Pipes
Which curve to use?
  Internal Pressure (Circumferential?)
  Lateral Loads (Longitudinal?)

## Slide 31: Material properties of hss pipes
Bauschinger Effect
Stress
Strain

## Slide 32: Material Properties of HSS Pipes
Manufacturing Process
Herynk, M.D.; Kyriakides, S.; Onoufriou, A. and Yun, H.D. (2007). Effects of the UOE/UOC pipe manufacturing processes on pipe collapse pressure. International Journal of Mechanical Sciences 49:533-553.

## Slide 33: Material Properties of HSS Pipes
Pipe Expansion (Circumferential Stress Strain Curve)
Stress
Strain

## Slide 34: Material Properties of HSS Pipes
Pipe Expansion (Circumferential Stress Strain Curve)
Stress
Strain
Stress

## Slide 35: Material Properties of HSS Pipes
Bauschinger Effect Model
Stress
Plastic Strain
Stress
Plastic Strain
Neupane, S.; Adeeb, S.; Cheng, J.J.R., Ferguson, J. and Martens, M. (2012). Modelling the deformation response of high strength steel pipelines, Part I: Material characterization to model the plastic anisotropy. ASME Journal of Applied Mechanics, 79(5):051002 (9 pages).

## Slide 36: Material properties of hss pipes
Anisotropy and Buckling
  Which curve should we use?
 | 0%SMYS | 80%SMYS
Circumferential |  | 
Longitudinal |  | 
Anisotropic model |  | 

## Slide 37: Material properties of hss pipes
Anisotropy and Buckling
Neupane, S.; Adeeb, S.; Cheng, J.J.R., Ferguson, J. and Martens, M. (2012). Modelling the deformation response of high strength steel pipelines, Part II: Effects of material characterization on the deformation response of pipes. ASME Journal of Applied Mechanics, 79(5):051003 (7 pages).

## Slide 38: Material properties of hss pipes
Anisotropy and Buckling
Neupane, S.; Adeeb, S.; Cheng, J.J.R., Ferguson, J. and Martens, M. (2012). Modelling the deformation response of high strength steel pipelines, Part II: Effects of material characterization on the deformation response of pipes. ASME Journal of Applied Mechanics, 79(5):051003 (7 pages).

## Slide 39: Material properties of hss pipes
Anisotropy and Buckling
  At high values of internal pressure, the circumferential stress strain curve governs buckling behaviour
  At zero internal pressure, the longitudinal stress strain curve governs buckling behaviour
Neupane, S.; Adeeb, S.; Cheng, J.J.R., Ferguson, J. and Martens, M. (2012). Modelling the deformation response of high strength steel pipelines, Part II: Effects of material characterization on the deformation response of pipes. ASME Journal of Applied Mechanics, 79(5):051003 (7 pages).

## Slide 40: Initial Imperfections of HSS Pipes
Initial Imperfections Measurement
(20micrometer + 25micrometer/meter)

## Slide 41: Initial Imperfections of HSS Pipes
Initial Imperfections Measurement
(20micrometer + 25micrometer/meter)

## Slide 42: Initial imperfections of hss pipes
Best Fit Cylinder
Kainat, M.; Adeeb, S.; Cheng, J.J.R.; Ferguson, J. and Martens, M.(2012). Identifying initial imperfection patterns of energy pipes using a 3D laser scanner. Proceedings of the International Pipeline Conference (IPC), September 24-28, Calgary, Alberta, Canada. IPC2012-90201.

## Slide 43: Initial imperfections of hss pipes
Initial Imperfection Measurements
Kainat, M.; Adeeb, S.; Cheng, J.J.R.; Ferguson, J. and Martens, M.(2012). Identifying initial imperfection patterns of energy pipes using a 3D laser scanner. Proceedings of the International Pipeline Conference (IPC), September 24-28, Calgary, Alberta, Canada. IPC2012-90201.

## Slide 44: Initial imperfections of hss pipes
Ovalization
Ovality =
Kainat, M.; Adeeb, S.; Cheng, J.J.R.; Ferguson, J. and Martens, M.(2012). Identifying initial imperfection patterns of energy pipes using a 3D laser scanner. Proceedings of the International Pipeline Conference (IPC), September 24-28, Calgary, Alberta, Canada. IPC2012-90201.

## Slide 45: Initial imperfections of hss pipes
Wall Thickness Measurement
Kainat, M.; Adeeb, S.; Cheng, J.J.R.; Ferguson, J. and Martens, M.(2012). Identifying initial imperfection patterns of energy pipes using a 3D laser scanner. Proceedings of the International Pipeline Conference (IPC), September 24-28, Calgary, Alberta, Canada. IPC2012-90201.

## Slide 46: Initial imperfections of hss pipes
Ovality Results
Kainat, M.; Adeeb, S.; Cheng, J.J.R.; Ferguson, J. and Martens, M.(2012). Identifying initial imperfection patterns of energy pipes using a 3D laser scanner. Proceedings of the International Pipeline Conference (IPC), September 24-28, Calgary, Alberta, Canada. IPC2012-90201.

## Slide 47: Initial imperfections of hss pipes
Ovality Results
Kainat, M.; Adeeb, S.; Cheng, J.J.R.; Ferguson, J. and Martens, M.(2012). Identifying initial imperfection patterns of energy pipes using a 3D laser scanner. Proceedings of the International Pipeline Conference (IPC), September 24-28, Calgary, Alberta, Canada. IPC2012-90201.

## Slide 48: Initial imperfections of hss pipes
Ovality Results
Kainat, M.; Adeeb, S.; Cheng, J.J.R.; Ferguson, J. and Martens, M.(2012). Identifying initial imperfection patterns of energy pipes using a 3D laser scanner. Proceedings of the International Pipeline Conference (IPC), September 24-28, Calgary, Alberta, Canada. IPC2012-90201.

## Slide 49: Initial imperfections of hss pipes
Wall Thickness Results
Upto 30% increase
Upto 15% decrease
Kainat, M.; Adeeb, S.; Cheng, J.J.R.; Ferguson, J. and Martens, M.(2012). Identifying initial imperfection patterns of energy pipes using a 3D laser scanner. Proceedings of the International Pipeline Conference (IPC), September 24-28, Calgary, Alberta, Canada. IPC2012-90201.

## Slide 50: Initial imperfections of hss pipes
Ovality vs. Wall Thickness Imperfections and Buckling

## Slide 51: Initial imperfections of hss pipes
Ovality vs. Wall Thickness Imperfections and Buckling
NPS 42, 14.275mm wall thickness. X100

## Slide 52: Initial imperfections of hss pipes
Ovality vs. Wall Thickness Imperfections and Buckling
and OR2 Imperfection Model
OR1 Imperfection Model
OR2 Imperfection Model

## Slide 53: Initial imperfections of hss pipes
Ovality vs. Wall Thickness Imperfections and Buckling
Wall Thickness Imperfection

## Slide 54: Initial imperfections of hss pipes
Ovality vs. Wall Thickness Imperfections and Buckling
Compare Ideal Pipe with:
 | 0%SMYS |  |  |  | 80%SMYS |  |  | 
OR1 |  |  |  |  |  |  |  | 
OR2 |  |  |  |  |  |  |  | 
WT |  |  |  |  |  |  |  | 
 | 0%SMYS |  |  |  | 80%SMYS |  |  | 
OR1 |  |  |  |  |  |  |  | 
OR2 |  |  |  |  |  |  |  | 
WT |  |  |  |  |  |  |  | 
x
Seam Weld
x
Seam Weld
y
Seam Weld
y
Seam Weld

## Slide 55: Initial imperfections of hss pipes
Oval vs. Ideal Pipe: No Difference!

## Slide 56: Initial imperfections of hss pipes
Wall thickness imperfection vs. Ideal Pipe:
x
Seam Weld
x
Seam Weld
y
Seam Weld
y
Seam Weld

## Slide 57: Initial imperfections of hss pipes
Wall thickness imperfection vs. Ideal Pipe:

## Slide 58: Initial imperfections of hss pipes
Wall thickness imperfection vs. Ideal Pipe:
Wall Thickness Deviation Model |  |  |  |  | 
 | Direction | Peak Moment | Difference | End Rotation | Difference
 | Of Rotation | (kN-m) |  | (Radians) | 
Without Pressure | Rx | 11401 | 4.72% | 0.1271 | 32.41%
 | R-x | 10254 | -5.81% | 0.0697 | -27.32%
 | Ry | 11211 | 2.97% | 0.1141 | 18.89%
 | R-y | 10411 | -4.37% | 0.0768 | -20.01%
With Pressure | Rx | 9647 | 22.88% | 0.1488 | 29.76%
 | R-x | 6305 | -19.69% | 0.1021 | -11.00%
 | Ry | 8950 | 14.00% | 0.1345 | 17.30%
 | R-y | 6880 | -12.37% | 0.1064 | -7.24%

## Slide 59: summary
In severe bending situations, internal pressure can cause rupture on the tension side!
HSS pipes have anisotropic behaviour which should be included for precise modelling
HSS pipeline imperfections are dependent on the UOE manufacturing process
Wall Thickness Imperfections can reduce the moment capacity by up to 20%
Wall Thickness Imperfections can reduce the critical strain by up to 27%

## Slide 60: Acknowledgements
Co-investigator:
  Dr. Roger Cheng.
  Chair, Civil and Environmental Engineering
Students:
  Sunil Neupane
  Muntaseer Kainat
  Celal Cakiroglu
  Meng Lin
Enbridge:
  Dr. Millan Sen
TCPL:
  Michael Martens
  James Ferguson
Funding:
  NSERC

## Slide 61: Questions
?